## Slide 1
Choosing the Right Architecturally Exposed Steel Category
Notes: Title Slide
Project:
Anaheim Regional Transportation Intermodal Center (ARTIC)
Anaheim, CA
2015 IDEAS2 Winner

## Slide 2
Learning Objective 1:
Discuss the expectations of fabrication and erection of exposed structural steel, standard & architectural, under the American Institute of Steel Construction’s 2016 Code of Standard Practice.
Learning Objective 2:
Understand how the increase in labor and craftsmanship required for higher categories of architecturally exposed structural steel affects project budgets.
Learning Objective 3:
Understand what steel fabrication options are available that can control project budgets while still providing a higher aesthetic product.
Learning Objective 4:
Identify available resources for information and specification language when utilizing exposed steel on existing and planned projects.
Learning Objectives

## Slide 3
History of Exposed Steel
Buyer Be-Aware
Steps to AESS Category Selection
Questions
Resources
Notes: Agenda for today’s presentation
Project:
Washington-Wabash ‘L’ Station
Chicago, IL
AISC photo

## Slide 4
History of Exposed Structural Steel
Notes: TRANSITION SLIDE
The use of architecturally expressive exposed steel dates back to the start of the shift of cast iron to structural steel.
Project:
Eiffel Tower
Paris, France
Pexel.com - Free photo service
Constructed from 1887–89 , the Eiffel Tower is a wrought iron building. And was the world’s tallest structure until the completion of the Chrysler Building in 1930.

## Slide 5
Notes: Modern use of architecturally exposed structural steel in the US is said to have started with Helmut Jahn’s United Airlines Terminal in Chicago in 1987, and since the usage of architecturally exposed structural steel (AESS) has spread to everything from small retail stores to office lobbies (quote 2003 AESS Brochure). And if you are visiting Chicago, you will see that the embracement of AESS has continued throughout the years.
Left:
United Terminal – Chicago O’Hare Airport
Chicago, IL
MSC image
Right:
Cermark-McCormic Place ‘L’ Station
Chicago, IL
IDEAS2 Entry

## Slide 6
Notes: Prior to 2016, previous codes and standards—even AISC’s Code of Standard Practice—do not fully address the unique level of detail needed to successfully design, detail, fabricate and erect Architecturally Exposed Structural Steel (AESS) projects.
And this was due to two reasons, one, there was a One-Size-Fits-All to structural steel. It was either standard structural steel as you see on the left, or it was architecturally exposed structural steel as you see on the right.
SLIDE TRANSITION
And because there was only one designation for AESS, expressive steel projects small to large with differing aesthetic approaches were treated the same.
Left:
7 Bryant Park
New York, NY
AISC photo
Center:
2010 AISC Code of Standard Practice
Right:
US Air Force Academy Center for Character and Leadership Development
Colorado Springs, CO
2018 IDEAS2 Winner
SLIDE TRANSITION
Left:
2010 AISC Code of Standard Practice
Center:
Lady Bird Lake Hike and Bike Trail Restroom
Austin, Texas
2011 IDEAS2 Award Winner
Right:
Brookfield Place Entry Pavilion
New York, NY
2014 IDEAS2 Award Winner

## Slide 7
BUYER BEWARE!
Unexpected Cost
Unexpected Look
Unclear Contract Language
Confusing Expectations
Good Luck!
Notes: This One-Size-Fits-All approach caused some confusion in the market. With many project teams feeling as if they should stamp Buyer Beware on the contract documents whenever AESS was mentioned. There was an immediate fear of cost overruns. The final look made some feel as if they were playing the telephone game with the steel fabricator and erector. And those who did not understand how to modify their contract specifications beyond the AISC Code of Standard Practice felt left out.
Thus, teams threw caution to the wind, crossed their fingers and either had great or not so great experiences with AESS.
Project:
Brookfield Place
Toronto, Canada
AISC Photo
Brookfield Place was one of the first AESS projects to use a category system. The team decided to use higher level craftsmanship at the base of the structure, and reduced the craftsmanship as the height of the structure increased. Thus, letting geometry not craftsmanship being the key behind the expressive roof lattice.

## Slide 8
SEA of Colorado Steel Liaison Committee
Rocky Mountain Steel Construction Association
Denver Architects
Denver Steel Suppliers
2002 AESS Collaboration
Notes: So while a number of project teams were feeling the AESS burn, a collaborative group in Denver, Colorado got together to create tools to help the design and construction industry better understand contract language and cost implications when using AESS.
Images:
Logos of some of the participants of the 2002 AESS Collaborative

## Slide 9
BEWARE -
Be Aware
COSP Requirements
Detailing Considerations
Fabrication Items
Erection Items
Communication
Cost of Craftsmanship
Notes: And in 2003 the group published their locally crafted tools in the May issue of Modern Steel Construction Magazine [Note this issue was one of the most downloaded of all time]
Listed are the items that teams were using outside of the Code of Standard practice to communicate the desired appearance for AESS. The brochure also included a conceptual cost tool that helped them to determine if AESS was within reach of their project. And for those groups who knew about the brochure, it was a great tool in approaching AESS projects and helped turn the feeling of BUYER BEWARE to Buyer Be Aware
Image:
2003 AESS Brochure
No longer in use
According to the Committee: “The goal of these tools is to allow the designer to communicate the desired appearance in a format that Contractors can price/budget/bid more appropriately.”

## Slide 10
AISC COSP
Section 10 - AESS
AESS 1
AESS 2
AESS 3
AESS 4
AESS C – Custom
Notes: The brochure and information contained within it was so successful, that AISC adopted the Collaborative’s AESS category system in the 2016 AISC Code of Standard Practice.
The AISC Code of Standard Practice for Steel Buildings and Bridges, an approved ANSI document AISC 303-16, implements a defined approach to specifying AESS in the contract documents by using five categories (AESS 1, 2, 3, 4, and C) to differentiate levels of steel fabrication and erection (see category matrix and image chart provided later in course).
Image:
2016 AISC Code of Standard Practice
As the numbers in this tiered system rise, the cost and time for fabrication and erection typically also increase. A similar approach was adopted in the Canadian Code of Standard Practice in 2009 with the CISC Code of Standard Practice for structural steel, seventh edition. Previous versions of the codes did not define the terms of AESS as distinctly, leaving room for interpretation and cost escalation. The 2016 document, AISC 303-16, may be referenced as a standard in contract documents prior to municipalities adopting it, the 2016 AISC Specification for Steel Buildings, and the 2018 International Building Code.

## Slide 11
New
2016-2018
Sample Specification
Cost Matrix
Shop Drawings
Architectural Record
Modern Steel Construction
Notes: And the Denver Collaborative was approached once again to revise, refresh, and expand upon the information they put together in 2002. And between 2016 and 2018, the Denver Collaborative in conjunction with AISC has published the listed materials.
A sample specification that helps with AESS contracts.
A conceptual cost matrix, which used a national pool of steel fabricators and erectors to help project teams better understand the cost impact of each category as well as the cost impact of certain fabrication and erection methods.
Shop drawings of the AESS samples to help groups prepare for fabrication documentation under the new category system
And AISC has published numerous articles in Architectural Record Magazine and Modern Steel Construction Magazine to reach out to general public and to again help bring awareness to the communication and cost tools for teams using the new AESS category system.
Image:
2017 AISC AESS Brochure (includes most items listed above)

## Slide 12
1
4
C
Notes: SUMMARY SLIDE
So now there is a mechanism that gives each unique exposed steel project the communication and budget controlling mechanism for success, regardless of size, shape, and desired finish.
Left:
Lady Bird Lake Hike and Bike Trail Restroom
Austin, Texas
2011 IDEAS2 Award Winner
Center:
Brookfield Place Entry Pavilion
New York, NY
2014 IDEAS2 Award Winner
Right:
US Air Force Academy Center for Character and Leadership Development
Colorado Springs, CO
2018 IDEAS2 Winner

## Slide 13
10 Step Category Selection System
Notes: TRANSITION SLIDE
So with a new code and publications, many people wonder how to use everything in their category selection process. And this portion of the presentation will go over the 10 steps to AESS Category selection.
Project:
World Trade Center Transportation Hub
New York, NY
2018 IDEAS2 Winner
AISC photo

## Slide 14
Steps to AESS Awareness
2016 AISC Code of Standard Practice
Industry Publications
AESS Fabricator Tips
Notes: The steps were created starting with a deep understanding of the 5 new AESS categories. Next we figured out a practical way to use all of the various publications. And finally as an added bonus, we asked steel fabricators who have worked with AESS what are friendly tips and reminders for project teams as they approach a new project. And the result is ten easy steps that can help project teams find the right mix of categories that fits their project budget. All while achieving the desired finish of the exposed steel.
Project:
Cruciform creation
IDEAS2 Entry

## Slide 15
AESS Categories
1
Notes: STEP 1:
The first step is to be aware the at teams now have six options to use for exposed steel projects.
Project:
Pomona College – Studio Art Hall
Claremont, CA
2015 IDEAS Winner

## Slide 16
Fabricator Friendly Tip
“Take the time to understand the different AESS levels and do not specify a higher level than necessary.”
Notes: And this is where the first fabricator tip starts. Reading through in depth the new categories is a must for project teams. We will not go through each category in depth today, but we will provide a quick overview so you can gain an idea of what to expect.

## Slide 17
Code of Standard Practice: Section 10
AESS 1: Basic elements
AESS 2: Feature elements viewed at a distance greater than 20 feet
AESS 3: Feature elements viewed at a distance less than 20 feet
AESS 4: Showcase elements with special surface and edge treatment beyond fabrication
AESS C: Custom elements with characteristics described in the contract documents
Notes: Here are the five new AESS categories. The sixth option I mentioned before is standard structural steel, which we will discuss later.
As you can see here the Code of Standard Practice outlines different intents for each category.

## Slide 18
Section 10 - AESS
AESS 1
AESS 2
AESS 3
AESS 4
AESS C – Custom
AESS 1
Notes: In NYC you will find mosaics in every subway station, and the murals on the new portion of the 2nd Avenue Subway line are great at explaining the intent of the new AESS categories.
Starting with category 1, the mosaics up close in this mural look a little crazy. You don’t know exactly what you are looking at, and there is no consistency to the level of finish of the various tiles.
Project:
86th Street Station
New York, NY
AISC photo

## Slide 19
AESS 1
Basic elements in AESS 1 are those that have workmanship requirements that exceed SSS
Notes: And that is because this installation is not meant to be seen up close, but at a distance. If you step back, portrait comes into view, and this is the thought behind AESS 1. We are treating the steel only slightly to provide a nice subtle level of expression that may not be apparent up close.
10.1.1. The following categories shall be used when referring to AESS:
AESS 1: basic elements
Commentary:
Basic elements in AESS 1 are those that have workmanship requirements that exceed what would be done in non-AESS construction.
Project:
86th Street Station
New York, NY
AISC photo

## Slide 20
AESS 1 – Basic Elements
Sharp edges ground smooth
Weld splatter shall be removed
Continuous weld appearance
Commercial Blast Cleaning (SSPC SP6)
Notes: This slide shows that as soon as you use any level of AESS, extra care and more labor is required of the steel fabricator and steel erector. This slide does not include all of the extra care and craftsmanship, but is a brief summary.
The key is that there is basic extra care being performed on the steel when compared to standard structural steel.

## Slide 21
AESS 1
Notes: AESS 1 Example : Here the steel is located well above the end users, and the shapes are simple and elegant and thus do not require extensive craftsmanship.
Project:
University of Texas at Dallas / Visitor Center and University Bookstore
Richardson, TX
IDEAS2 Entry

## Slide 22
AESS 1
Notes: AESS 1 Example : Canopies are a nice example of using lower levels of AESS. For this project only a small amount of craftsmanship is needed to help the various canopy materials and lighting come together. The end user again is not looking directly at connections, but from distance and over the aesthetic is more than just standard structural steel.
Project:
Knox Building Canopy Restoration
New York, NY
IDEAS2 Entry

## Slide 23
AESS 2
Notes: Back to the mosaics in the subway, here we are up close again looking at the tile of the mural. Now we see a little more craftsmanship in the tile shape, slightly more consistency in the surface finish, but again up close we are not able to appreciate the desired aesthetic.
Project:
86th Street Station
New York, NY
AISC photo

## Slide 24
AESS 2
Achieved primarily through geometry without finish work
Notes: With this mural you are again viewing the subject at a distance, and unlike AESS 1 geometry is used more to create a more dynamic and enhanced look.
10.1.1. The following categories shall be used when referring to AESS:
AESS 2: feature elements viewed at a distance greater than 20 ft (6 m)
Commentary:
Feature elements in AESS 2 and 3 exceed the basic requirements, but the intent is to allow the viewer to see the art of metalworking. AESS 2 is achieved primarily through geometry without finish work, and treats things that can be seen at a larger viewing distance, like enhanced treatment of bolts, welds, connection and fabrication details, and tolerances for gaps, copes and similar details.
Project:
86th Street Station
New York, NY
AISC photo

## Slide 25
AESS 2 – Feature Elements (> 20 feet)
One-half the standard fabrication tolerances
Fabrication and erection marks not apparent
Welds uniform and smooth (not ground smooth or contoured)
Notes: And in addition to the extra craftsmanship included in AESS 1, more levels of craftsmanship are added as each category increases. The extra craftsmanship for AESS 2 while greater than AESS 1 is not intended to be viewed up close, so for projects well above 20 feet this level of craftsmanship is just right.

## Slide 26
AESS 2
Notes: AESS 2 Example - Austin Bergstrom Airport
For this project, the exposed steel is 50 ft above the concourse floor. Thus the welds are not immediately visible by the naked eye, and the project team can focus on tolerances and geometry to complete the look. (Note, when visiting this installation, up close the welds are not ground down and are made to look uniform.
Project:
Terminal East Infill at Austin-Bergstrom International Airport
Austin, Texas
2017 IDEAS2 Winner

## Slide 27
AESS 2
Notes: AESS 2 Example : The geometry of this roof structure takes center stage as the star and not the steel connections. Thus, the roof portion of this project would work well as a AESS 2 example
Project:
The Oratory at Ave Maria
Ave Maria, FL
2008 IDEAS2 Winner
Cannon Design Photo

## Slide 28
AESS 3
Notes: Back to the mosaics. Now the installations are meant to be seen at a closer view. Here you see more detail coming into play, the shape of the mosaics no longer catches the eye, arrangement and paint brush strokes become the focus.
Project:
86th Street Station
New York, NY
AISC photo

## Slide 29
AESS 3
Achieved through geometry and basic finish work
Notes: And regardless of whether you are up-close or far away, you can see the craftsmanship. The geometry and craftsmanship together create an enhanced aesthetic.
10.1.1. The following categories shall be used when referring to AESS:
AESS 3: feature elements viewed at a distance less than 20 ft (6 m)
Commentary:
Feature elements in AESS 2 and 3 exceed the basic requirements, but the intent is to allow the viewer to see the art of metalworking…AESS 3 is achieved through geometry and basic finish work, and treats things that can be seen at a closer viewing distance or are subject to touch by the viewer, with welds that are generally smooth but visible. AESS 3 involves the use of a mockup and acceptance is based upon the approved conditions of the mock-up.
Project:
86th Street Station
New York, NY
AISC photo

## Slide 30
AESS 3 – Feature Elements (< 20 feet)
Visual samples (mock-up) required
Mill marks removed
Butt and plug welds ground smooth and filled
HSS weld seam oriented for reduced visibility
Cross sectional abutting surface aligned
Open joint gap tolerances minimized
Notes: Here is a summary of the additional items added on top of the items that we saw with both AESS 1 and AESS 2. All of the items are made to give projects closer to the end user a nicer finish. One key item to note with AESS 3 is that project teams will now be required to have a visual sample created of a portion of the AESS installation. As the steel will be close with the craftsmanship visible to the naked eye, the mock-up is necessary to ensure that the design and steel teams agree on the craftsmanship prior to the entire project being fabricated.

## Slide 31: AESS 3
Notes: AESS 3 Example. The black façade that you see here is all exposed structural steel. The columns are created using steel plate, and the fabricator used a robotic welding process that creates smooth welds that while still visible are clean and nice to touch.
Project:
Fulton Center
New York, NY
2017 IDEAS2 Winner

## Slide 32: AESS 3
Notes: AESS 3 Example : Here the steel is very close to the end user, and the geometry and clean connections lend well to the structure.
Project:
Pterodactyl Office Building
Culver City, CA
2017 IDEAS2 Award Winner

## Slide 33
AESS 4
Notes: And at this level, passerby's are actually encouraged to touch the mosaics as they have texture different finishes (glossy and matte) true details that are to be explored. The tiles themselves become the background with the details becoming more of the feature.
Project:
86th Street Station
New York, NY
AISC photo

## Slide 34
AESS 4
The form is the only feature showing in an element
Notes: And at this level the tiles used to create the mural fade into the background and become secondary to the overall aesthetic. This is the intent for AESS 4, the overall form will be the feature, and at time people will not realize that they are looking at structural steel.
10.1.1. The following categories shall be used when referring to AESS:
AESS 4: showcase elements with special surface and edge treatment beyond fabrication
Commentary:
Showcase elements in AESS 4 are those for which the designer intends that the form is the only feature showing in an element. All welds are ground and filled, edges are ground square and true. All surfaces are filled and sanded to a smoothness that doesn’t catch on a cloth or glove. Tolerances of fabricated forms are more stringent—generally half of standard tolerance. AESS 4 involves the use of a mock-up and acceptance is based upon the approved conditions of the mock-up.
Project:
86th Street Station
New York, NY
AISC photo

## Slide 35
AESS 4 – Showcase Elements
Visual samples required
Weld contoured and blended
Surfaced imperfections filled and sanded to meet visual sample criteria
Weld show-through minimized
HSS seams treated
Notes: In summary all of the items from AESS 1, AESS 2, and AESS 3 are included with AESS 4 with extra craftsmanship included.

## Slide 36
AESS 4
Notes: AESS 4 Example : Here for this residential project, you can see the steel “trees” look as if they were cast or extruded
Project:
Fischer House
Fischers Island, NY
2010 IDEAS2 Award Winner

## Slide 37
AESS 4
Notes: AESS 4 Example : Probably a new classic example of the form of the project taking center stage is the new WTC Transportation Hub which is created entirely from steel plate and is fabricated and erected in such a way that it looks like cast construction.
Project:
WTC Transportation Hub
2018 IDEAS2 Winner
New York, NY
Photo: AISC

## Slide 38
AESS C
Notes: And thinking about a custom approach, as you can see here there are various levels of craftsmanship and finish, as it is up to the specifier (or artist in this case) to create the desired look.
Project:
72nd Street Subway Station
New York, NY
AISC photo

## Slide 39
AESS C
Custom elements with characteristics described in the contract documents
Notes: And this category allows you to select what level of craftsmanship best fits your budget and aesthetic for the project. Every example that you have seen thus far could use the Custom Category system, the design team would just define their needs in easy contract language for the steel team to understand.
10.1.1. The following categories shall be used when referring to AESS:
AESS C: Custom elements with characteristics described in the contract documents.
Commentary:
Custom elements in AESS C are those with other requirements defined in the contract documents.
Project:
72nd Street Subway Station
New York, NY
AISC photo

## Slide 40
 |  | AESS C | AESS 4 | AESS 3 | AESS 2 | AESS 1 | SSS
 |  | Custom | Showcase | Feature | Feature | Basic | Standard
 |  | Elements | Elements | Elements in | Elements not | Elements | Structural
ID | Characteristics |  |  | close view | in close view |  | Steel
1.1 | Surface preparation to SSPC-SP 6 |  | ● | ● | ● | ● | 
1.2 | Sharp edges ground smooth |  | ● | ● | ● | ● | 
1.3 | Continuous weld appearance |  | ● | ● | ● | ● | 
1.4 | Standard structural bolts |  | ● | ● | ● | ● | 
1.5 | Weld spatters removed |  | ● | ● | ● | ● | 
2.1 | Visual samples | mock-up required | mock-up required | mock-up required | optional |  | 
2.2 | One-half standard fabrication tolerances |  | ● | ● | ● |  | 
2.3 | Fabrication marks not apparent |  | ● | ● | ● |  | 
2.4 | Welds uniform and smooth |  | ● | ● | ● |  | 
3.1 | Mill marks removed |  | ● | ● |  |  | 
3.2 | Butt and plug welds ground smooth and filled |  | ● | ● |  |  | 
3.3 | HSS weld seam oriented for reduced visibility |  | ● | ● |  |  | 
3.4 | Cross sectional abutting surface aligned |  | ● | ● |  |  | 
3.5 | Joint gap tolerances minimzed |  | ● | ● |  |  | 
3.6 | All welded connections |  | optional | optional |  |  | 
4.1 | HSS seam not apparent |  | ● |  |  |  | 
4.2 | Welds contoured and blended |  | ● |  |  |  | 
4.3 | Surfaces filled and sanded |  | ● |  |  |  | 
4.4 | Weld show-through minimized |  | ● |  |  |  | 
C.1 |  |  |  |  |  |  | 
C.2 |  |  |  |  |  |  | 
C.3 |  |  |  |  |  |  | 
Notes: With the Custom Category you will fill out your project needs within the Matrix (Table 10.1 and available online) that has the fabrication and erection considerations for AESS 1, AESS 2, AESS 3, and AESS 4 listed, and the matrix has blank custom items for your team to write in additional considerations for your AESS project.
Image: Excel created copy of Table 10.1

## Slide 41
AESS C
Notes: AESS C Example : This project is great example of a custom category in that wood has differing tolerances for fabrication and erection when compared to steel. To ensure that both materials are received the desired craftsmanship for the hybrid look, the Custom category matrix would help to communicate the steel’s needs.
Project:
U.S. Army Corps of Engineers – Federal Center South Building
SEATTLE, WASH.
2014 IDEAS2 Award Winner

## Slide 42
AESS C
Notes: AESS C Example : Here the rustic design does not require a lot of craftsmanship. And if the project team requires some craftsmanship that exceeds standard structural steel, but does not need as much as the considerations for AESS 1 (e.g. SSPC 6), then the Custom category is great to use. Simple select the few items necessary and the fabricator and erector will be on the same page. Even with a mock-up the project is simplified and the desired finishes are achieved.
Project:
LAMAR STATION - A CLASSROOM FOR URBAN FARMING
Lakewood, CO
2018 IDEAS2 Winner

## Slide 43
Cost of Craftsmanship
2
Notes: STEP 2
Understanding the cost of craftsmanship. And this digs into the question that people ask the most…”How much is a ton of steel?” and the answer “It depends” because there are so many levels of workmanship being performed from one project to the next.

## Slide 44
Fabricator Friendly Tip
“Do not assume that an AESS project will have the same cost as a Walmart store.”
Notes: The first thing to understand is that AESS projects will not have the same cost as low level craftsmanship projects.

## Slide 45
Notes: And while it may seem that this should go without saying, we have seen instances where groups will take the same price per ton for fabrication or erection of a standard school project and apply it to an AESS project. In this example the scaffolding alone should alert you to the extra work and equipment needed for the project on the right.
Left:
Brearly Private School
New York, NY
AISC Photo
Right:
US Air Force Academy Center for Character and Leadership Development
Colorado Springs, CO
2018 IDEAS2 Winner

## Slide 46
Standard Steel Labor
Chart: 
| Labor | Material
 | 60 | 40
+60%
Notes: The fundamental factor to understand is that labor is always the largest portion of the cost of a structural steel framed building.
For a standard structural steel building, only 40% of the steel package cost is related to material (purchasing of shapes), the majority of the steel package cost +60% is in labor (fabricator, erector, etc.). Yes even with the current tariffs.
Embedded doughnut chart (change values or color if like)
Project:
MGM National Harbor
Oxon Hill, MD
AISC photo

## Slide 47
AESS Labor
Chart: 
| Labor | Material
 | 90 | 10
+90%
Notes: With AESS, will essentially become the entire cost of the steel package as craftsmanship not materials take center stage. As an example with the AESS 4 project example, the steel material would only be about 10% of the steel package – so 90% of the steel package cost is for the labor and added equipment to complete the extra labor.
Embedded doughnut chart (change values or color if like)
Project:
WTC Transportation Hub
2018 IDEAS2 Winner
New York, NY
Photo: AISC

## Slide 48
Fabricator Friendly Tip
“The design team needs to recognize that they will pay more for AESS and complex structures.”
Notes: And fabricators will point out that complex projects (even standard structural steel complex projects) and projects using the AESS category system will cost more than a simple SSS project.

## Slide 49
Range in Cost Increase Above SSS
AESS 1 | 10% - 20% | low
AESS 2 | 25% - 35% | low to moderate
AESS 3 | 40% - 75% | moderate
AESS 4 | 100% - 150% | high
AESS C | XX% to XX% | low to high
Notes: With the information provided by fabricators and erectors we can see that at a glance there is a range of additional cost when comparing each of the categories to a simple standard structural steel project.
For AESS 1, we see that project teams can expect an overall increase in steel package cost of 10 to 20 percent. And the ranges are there to give flexibility in items that the fabricator cannot control, such as sales or city taxes from area to area.
As the categories increase from 1 to 4 you can see how the extra craftsmanship impacts the overall budget. And it should be noted, that because you are creating your own category with AESS C, the cost will vary from anything below AESS 1 to something substantially more than AESS 4.
Image: Excerpt from Cost Matrix

## Slide 50
Primer & Finish Coatings
Finish A: Interior Environment - low end finish | 5% - 15%
Finish B: Interior environment - high end finish | 15% - 30%
Finish C: Exterior environment - low end finish | 20% - 40%
Finish D: Exterior environment - high end finish | 30% - 50%
Finish E: Galvanizing | 20% - 40%
Notes: And as an added bonus, the Cost Matrix includes general cost information for other items that impact the cost of an AESS structure. As an example, here are the ranges for finishing the steel with a coating.
Image: Excerpt from Cost Matrix

## Slide 51
Standard Steel
3
Notes: STEP 3
And this step is what I like to call the beauty of Standard structural steel. Because this is where you will decide if you really really really need to use AESS for the project.
There is a lot of beauty in standard structural steel. Geometry and proportion can turn simple projects into dazzling displays of design. And all without the use of adding extra craftsmanship. I love this example because the steel you see here is as basic as it gets, fabrication, mill, and erection marks included. But as you can see it works!
COSP 10.1 General Requirements Commentary
The designation of steel as AESS adds cost, and that cost is higher as the level of the AESS designation increases. However, not all exposed steel must be designated as AESS. There are many applications in which the as-produced appearance of fabricated and erected structural steel may be deemed sufficient without any special additional work.
Project:
Stanley Market Place
Aurora, CO
AISC Photo

## Slide 52
Fabricator Friendly Tip
“Many people consider all exposed steel to be AESS. This is not true or necessary.”
Notes: Ultimately the reminder is that all exposed steel is not architecturally exposed steel. It is in fact nice pieces of steel, with great geometry, given a corrosion protection system depending on it’s environment.
In depth with Larry Kruth, AISC - The biggest issue is for everyone to understand first the difference between exposed steel and AESS. Many people consider all exposed steel to be AESS. This is not true or necessary. If AESS is required all parties should pay close attention to all the levels of AESS in the COSP. This is a great improvement. Also, it is good to keep in mind that AESS C is not just for highly finished steel. For example, if you would like an AESS 2 but do not need an SSPC SP-6 finish, You could specify an AESS C to meet the requirements of AESS 2 with SSPC SP-3 finish.

## Slide 53
Visibility
Notes: If the steel is not visible, as we see with the roof steel for this canopy, then just use standard steel.
Project:
San Bernardino Transit Center
San Bernardino, CA
IDEAS2 Entry

## Slide 54
Setting
Notes: Another thing to think about is the setting. So on the left, if a person climbs this very extensive rock wall, I can guarantee that they are not looking at the welds on the joist to see if they are ground down and smooth.
And on the right, you can see that almost every person in the photo is looking at their phone and not the steel. So in both cases the steel is not the focal point. But not to pick on the university students on the right. They could actually be future architects and engineers, and in that case, it would be great to have steel in it’s nearly raw form as an education tool.
Left:
YWCA Sun ‘N Fun Outdoor Aquatics Center
Lubbock, TX
IDEAS2 Entry
Right:
The Collegiate Center at Edison
Tulsa, OK
IDEAS2 Entry

## Slide 55
Audience
Notes: And audiences can appreciate steel that is not fully exposed. In this photo, this is the ceiling of a structural engineering firm. The visualization helps them to understand the projects they are putting together, and the lighting helps to minimize imperfections at first glance.
Project:
Silman Consulting Engineers
New York, NY
AISC photos

## Slide 56
Style
Notes: Style is also important. This expansion project went with a simple design that did not require AESS. If you are not going with a plastic design where the steel look like it is extruded or cast from one piece, and if you are using shapes at eye level that do not require extra craftsmanship (such as HSS), then standard steel is all you need for an exposed steel application.
Project:
American Physical Society
Ridge, NY
2016 IDEAS2 Winner

## Slide 57
Visual AESS Mapping
4
Notes: STEP 4 :
The next step is for those who have decided that SSS will not provide the craftsmanship necessary for their project. And the start of selecting your AESS category is to first visually map where the categories would be used for your project.
Project:
US Air Force Academy Center for Character and Leadership Development
Colorado Springs, CO
2018 IDEAS2 Winner

## Slide 58
Notes: So using the renderings of you project. Grab your team and determine visually where you should spend the money on extra craftsmanship. So for this example, we see exposed steel at the roof, however, natural lighting from above, lighting from below and the screen system hinder the view of craftsmanship. Therefore, the project team can save money and just use standard structural steel for this application. Next we move onto the columns. And you can see that they columns have tapered ends and are within view of the end user. Therefore, we want to use AESS 3 for the column (and feel free to use AESS 2 at the top of the columns and AESS 4 at the bottom depending on the look that you want).
Project:
Weber County Library Headquarters Branch
Roy, UT
2017 IDEAS Winner

## Slide 59
AESS Budget Mapping
5
Notes: STEP 5
After you have visually mapped your desire for the AESS categories on the project. The next step is the map the budget of the project.
Image:
Pexel.com - Free photo service

## Slide 60
Fabricator Friendly Tip
“Least Weight ≠ Least Cost”
Notes: First understand that a lighter project does not automatically guarantee a cheaper project.

## Slide 61
AESS Labor
Chart: 
| Labor | Material
 | 90 | 10
+90%
Notes: As we discussed before, labor comprises a majority of the steel package for any steel projects. And higher levels of AESS or a complex Custom matrix can cause the labor to exceed 90% of the steel package. Thus, avoid using lighter materials as a means to save money, you may actual cause more labor for the steel (e.g. adding stiffner and doubler plates).
Project:
Fulton Center (built-up columns with smooth welds)
New York, NY
2017 IDEAS2 Winner

## Slide 62
Fabricator Friendly Tip
“Put your money only where it counts. The lowest possible AESS category should be specified to meet the project requirements.”
Notes: Ultimately make you budget stretch by adding craftsmanship only where needed.

## Slide 63
Notes: So as an example, lets say we wanted to use AESS 3 across this entire project. But after budget mapping we found that we would exceed our budget.
The next step would be to go back and fine tune the categories necessary. Since we are using castellated beams that are bolted, lets have the steel’s geometry take center stage and paint the steel a lighter matte color to hide imperfections. We can then classify the castellated beams as standard structural steel. Then we can spend a majority of our budget on the brace connection point using a Custom Category that focuses on the welds.
Project:
NY Police Academy
New York, NY
AISC Photo

## Slide 64
Think Like an Ironworker
6
Notes: STEP 6
The next step is to think like an ironworker.
Ironworkers in the field are part of the labor component of the steel package. So think about their process when you fine tuning the design and budget.
Project:
UC Davis Jan Shrem and Maria Manetti Shrem Museum of Art
Davis, CA
2018 IDEAS2 Winner

## Slide 65
Fabricator Friendly Tip
“AESS fieldwork is harder to achieve than shop work, so specify that as much work as practical is performed in the shop.”
Notes: Anything that can be done at ground level under a roof is always better for a project. And in addition to making welding and bolting easier, you avoid weather delays as well as slow downs due to extreme temperatures (too cold to work or too hot to work efficiently)

## Slide 66
Notes: If you’ve never performed an overhead weld, just imagine spending hours with your body angled upward with molten material flying at your person. And while many accomplish this process safely and with excellent results, understand that something as simple as ergonomics can add extra labor time and cost to your project.
Project:
UC Davis Jan Shrem and Maria Manetti Shrem Museum of Art
Davis, CA
2018 IDEAS2 Winner

## Slide 67
Notes: For projects that are projected to have heavy field labor, the project team may want to panelize portions of the project, or deliver the project to site in modules. Many project teams have benefitted from using offsite fabrication and assembled component transport to aid in the constructability of projects. This helps to reduce complex ironworker gymnastics, and can reduce the amount of time spent on the project as now you are welding, bolting, and fitting in a controlled environment.
For this example you can only image the ironworkers have to weld overhead each of the over 50 columns on site. Doing everything at an ergonomic level in the shop, helps the steel portion of construction last days instead of weeks.
Project:
Minnesota Fallen Firefighters Memorial
Saint Paul, MN
2015 IDEAS2 Award Winner

## Slide 68
Fabricator Friendly Tip
“Bolt (instead of weld) in the field where at all possible.”
Notes: Bolting instead of welding is overall a more economical approach for all steel to steel connections.

## Slide 69
Notes: And while there are many welders who can essentially weld in their sleep, there is still the need to have welding equipment nearby to perform the weld.
If an ironwork is having to work in complicated positions, it’s a lot easier to carry just one power tool (as you see here for bolting) instead of the extensive gear for welding.
This is essentially why you rarely see steel trusses erected in the field.
Project:
Arthur Ashe Stadium – US Open
New York, NY
IDEAS2 Entry

## Slide 70
Connections
7
Notes: STEP 7
So now that you have determined the connection type and where it will be welded or bolted together, the next step is to think about what the connections will look like. And this is also a place where you can reduce the AESS category if needed.
So here you can see some very aggressive looking welds, but they are okay because only pigeons and maintenance staff will be on the roof to view the connection. SSS or AESS 1 are fine for this rarely viewed connection.
Project:
1812 North Moore Street
Arlington, VA
AISC photo

## Slide 71
Notes: Also understand that welds can be made to look continuous without extra weld material.
On the left you see what is known as an Intermittent weld. It starts and stops on purpose because sometimes continuous welds can cause forces to go in strange places.
The weld can be made to look continuous like the weld on the right by using filler material instead of extra weld. This saves money and ensures that the proper welds are used.
Images: AESS Samples SSS and AESS 2

## Slide 72
Notes: With AESS projects it is also very important to spend extra time talking about bolts. On the right you see a strange display of the two bolt heads that are available for structural steel (hex head and button head). If you do not express which type of bolt head you would like you may end up surprised in the end. If you want button headed bolts make sure it is in the contract documents.
In the middle you will see the bolt head and nuts facing different directions. With the new category system all the heads will face the same direction so you do not have to worry about this. But consider the work of the ironworker when you are determining which direction to go.
On the right is a nice example of the bolt heads facing the same direction round the column. It’s nice and clean, and you can see that there is space for the wrench to reach the bolts as the ironworker moves around the column.
Left:
Times Square Subway Station
New York, NY
AISC Photo
Middle:
SoHo Uniqlo Department Store
New York, NY
AISC photo
Right:
SoHo Nike Store
New York, NY
AISC Photo

## Slide 73
Finalizing Finishes
8
Notes: STEP 8
Think about the corrosion project system you are using and make sure the steps necessary for high performance of the coating are expressed in the contract documents.
AESS 1, 2, 3, and 4 have a default surface preparation, SSPC SP6 – Commercial Blast Cleaning. This cleaning method removes most mill scale giving you a cleaner piece of steel. However, this cleaning method may actually make your steel too smooth for the paint to adhere. So triple check you paint specification and ensure that the right surface preparation method is being used for your project.
Project:
Landscape Evolution Observatory at Biosphere 2
Oracle, AZ
2015 IDEAS2 Winner

## Slide 74
Fabricator Friendly Tip
“Glossy coats tend to show every imperfection and surface variation”
Notes: So if you ever wonder why wall of apartments are always a light matte color, this is the reason why. Glossy and dark colors will show surface imperfections. If you want to use a lower category and hide imperfections think about a lighter matte color.
If you are using a heavy coating (such as intumescent paint) the coating will actually serve to hide some of the imperfections. So use color and coating selection to help reduce craftsmanship for your project.

## Slide 75
Notes: This is an example of dark glossy coats on the AESS sample.
On the right is AESS 2, and the glossy paint really makes the weld show through.
On the left is AESS 4, which looks fine because there is extra craftsmanship to ensure a nice smooth finish.
Therefore, if you really want to go for that super dark high gloss finish you may want to switch to a higher category, especially if the steel is at eye level.
Images
AESS Samples 2 and 4

## Slide 76
Fabricator Friendly Tip
“Consider applying the final coat of paint in the field because field touchup can leave blotches.”
Notes: The fabricator and erector are going to take extra care with AESS to ensure that the steel is not damaged or deformed during fabrication and erection. They are not necessarily looking out for the final coat of paint.
Therefore to avoid the potential of touch up spots standing out, fabricators and erectors advise that the final coating be applied in the field. The primer can be applied in the shop or offsite.

## Slide 77
Weathering Steel
Notes: If you are using weathering steel, we are going to suggest that you use Category C.
Starting with AESS 1 there is a default surface preparation of SSPC S6. If you want a very rustic look for weathering steel you many not want any surface preparation at all. And if you advancing the formation of the patina on the steel, again you may require a different surface preparation technique. So if you are working with weathering steel just default to Custom Category C to help communicate the final look of the weathering steel.
Project:
Central Arizona College Maricopa Campus
Maricopa, AZ
2015 IDEAS2 Winner

## Slide 78
Galvanizing
Notes: We also recommend you use Custom Category C for galvanized steel as well. The galvanization process has a distinct surface preparation as part of the process. To avoid extra craftsmanship use the custom category and eliminate the default SSPC SP6.
Project:
San Diego Public Library
San Diego, CA
AISC photo

## Slide 79
Contract Documents
9
Notes: STEP 9
So now that you have settled on the categories that fit the look and budget for your project. The next step is to ensure that all of the items are located in your contract documents. If you communicate everything effectively in the documents you will receive bids that are in line with the final product, and you will avoid miscommunication as the project progresses from procurement, to fabrication, to erection.
Image:
Pexel.com - Free photo service

## Slide 80
Fabricator Friendly Tip
“The AISC Steel Solutions Center sees a lot of situations where the parties assume that some condition is addressed in the Code of Standard Practice when it is not.”
Notes: In the past there were a lot of assumptions about what the craftsmanship would be for the one-size-fits-all AESS designation. As we saw with Step 1, make sure that you understand the level of craftsmanship for AESS 1, 2, 3, and 4. And make sure any craftsmanship not expressed in those categories is documented in Custom Category C.

## Slide 81
Contract & Approval Documents
Clear identification of AESS steel using the 5 categories
Indicate more restrictive tolerances
AESS C requires use of the AESS matrix
Identify variations from the COSP
Orientation of HSS weld seams
Direction of bolt heads
Notes: Here are just a few of the basic items that you will need to have to effectively communicate using the new category system.

## Slide 82
Sample AESS Specification
Section 05 12 13
Architecturally Exposed Structural Steel
Notes: And to help project teams write the specification, AISC along with the Denver Collective have updated the Sample Specification, and it includes sample language for all 5 categories.
Sample Specification available as Word Doc online (aisc.org/aess)
Image:
2017 AESS Brochure

## Slide 83
Ask the Steel Industry
10
Notes: And Finally STEP 10
The easiest step, ask a fabricator
Structural Steel fabricators have a wealth of knowledge that they are happy to share free of cost for project teams. There are hundreds of fabricators here who can help to answer your questions and help with the visual and budgeting mapping of your project.
Project:
425 Park Avenue Transfer Column at Owen Steel
Columbia, SC (Project in NY, NY)
AISC Photo

## Slide 84
Fabricator Friendly Tip
“If you get low prices on difficult or complex work, ask questions. It may be that the requirements have not adequately been conveyed or interpreted.”
Notes: If you are using design bid build as a delivery method and you receive a bid that is half that of the other steel teams, you may want to ask questions before you jump to the cheaper option. They may not be familiar with the work, or you may have missed communicating something in the initial documents.

## Slide 85
Fabricator Friendly Tip
“The biggest thing they can do is to bring the fabricator into the process early and communicate with the fabricator. They will know better than anyone else what the cost impacts of various options will be.”
Notes: And bringing your fabricator to the table for the project as early as possible helps any steel project (SSS or AESS). The fabricator has a wealth of material, labor, and constructability knowledge that you can unlock of overall project cost and schedule savings.

## Slide 86
10 Steps to Category Selection
New AESS Categories
Cost of Craftsmanship
Standard Steel
Visual Mapping
Budget Mapping
Ironworker Friendly
Connections
Finishes
Contracts
Ask a fabricator
Notes: SUMMARY SLIDE
In summary, putting these 10 steps together will help guide your project team in the selection of the six options available for exposed steel.

## Slide 87
Questions
Notes: TRANSITION SLIDE
Now we will open the presentation up for questions.
Project:
Rutgers University School of Business
Piscataway, NJ
2016 IDEAS2 Winner

## Slide 88
Notes: Are stairs made with structural shapes included in the AESS categories: NO
Project:
Artquest Center at Steel Stacks
Bethlehem, PA
IDEAS2 Entry

## Slide 89
Other Items
Cables
Castings
Handrails
Ornamental framing
Stairs
Notes: In Section 2 of the COSP you will find a list of what is and what is not considered structural steel. The listed items are those that many confuse with structural steel. And we understand that many of these items are created using structural material. However, they are not considered structural steel in the COSP and therefore the AESS categories that we just discussed do not apply.
If you would like to use the category system for Other items, you can simply create a category system within the specification for those items. E.g. a category system in the Misc. metals section.
Photo:
Smithsonian National Museum of African American History & Culture
Washington, DC
2017 IDEAS2 Winner

## Slide 90
Notes: Question:
Can I use the category system on exposed stainless steel?
NO
Project:
Fulton Center (stainless steel netting)
New York, NY
2017 IDEAS2 Winner

## Slide 91
Design Guide 27
Design
Practical Fabrication
Installation
Notes: Stainless steel is considered an “Other” material in the COSP.
And similar to stair you will have to create a category system within the Stainless Steel Specification.
AISC does in fact have a stainless steel design guide that includes tips for practical fabrication and installation. So if you are using the 10 steps for stainless steel, keep this in mind when you get to the Think like an Ironworker section.
Image:
AISC Design Guide 27

## Slide 92
Resources
Notes: TRANSITION SLIDE
Forground:
The Shed
New York, NY
AISC Photo
Background:
The Vessel
New York, NY
AISC Photo

## Slide 93: aisc.org/aess
Notes: www.whysteel.org is the main site and the shortcut is aisc.org/aess

## Slide 94: AESS Samples
Notes: And there are five samples available for your use on your next project
SSS
AESS 1
AESS 2
AESS 3
AESS 4
(there is no sample for custom category C)